|  |  |  |
| --- | --- | --- |
| Customer | Dal Tile |  |
| Sample ID | QUARTZ SAND ROOF-OK. Comp637 |  |
| Test | AGGREGATES CHARACTERIZATION |  |
| Sample (g) | 300 |  |
| Lab address | PF Lab Services – Simbario (VV) – ITALY |  |

|  |  |
| --- | --- |
| CHEMICAL COMPOSITION:QUARTZ SAND |  |
|  |  |
| MOISTURE CONCENTRATION: 0 % |  |
|  |  |
| Particles size distribution |  |
|  |  |
| Particles size analysis |  |
| |  |  | | --- | --- | | Diameter (µm) | Passing (%) | | 500 | 99,98 | | 355 | 99,65 | | 212 | 75,02 | | 125 | 11,97 | | 80 | 0,55 | | 63 | 0,09 | |  |  | |  |
| For the analysis were used Sieves mesh mall S Steel I.S.O. 3310 (UNI EN 933-2) and electric sieve shaker with timer (UNI EN 932-5 ISO 3310-1). |  |