|  |  |  |
| --- | --- | --- |
| Customer | Colorificio Lentini |  |
| Sample ID | Sabbia Petrizzi |  |
| Test | AGGREGATES CHARACTERIZATION |  |
| Sample (g) | 330 |  |
| Lab address | PF Lab Services – Simbario (VV) – ITALY |  |

|  |  |
| --- | --- |
| CHEMICAL COMPOSITION: SABBIA STILO |  |
|  |  |
| MOISTURE CONCENTRATION: 0% |  |
|  |  |
| Particles size distribution |  |
|  |  |
| Particles size analysis |  |
| |  |  | | --- | --- | | Diameter (µm) | Passing (%) | | 850 | 82.81 | | 710 | 77.00 | | 600 | 68.79 | | 500 | 60.69 | | 300 | 44.73 | | 212 | 25.39 | | 125 | 12.37 | | 80 | 6.30 | | 63 | 3.96 | |  |
| For the analysis were used Sieves mesh mall S Steel I.S.O. 3310 (UNI EN 933-2) and electric sieve shaker with timer (UNI EN 932-5 ISO 3310-1). |  |